动力锂离子电池产品规格书

PowerLithium-IonbatterySpecification

| 型号/Model | LFP30L-BS |
| --- | --- |
| 客户名称/ Customer |  |
| 文件编号/Document NO. |  |
| 发行日期/Issue Date | 2020-10-27 |

| 制定 / Preparedby | 审核 / Checkedby | 批准 / Approvedby |
| --- | --- | --- |
| 王立峰 | 贾小刚 | 张彬 |

目录/ContentsPage

封面 Cover

目录Catalogue-----------------------------------------------------1

1、适用范围Scope-------------------------------------------------  3

2、电池组特性 Battery Group Specifications------------------------  3

3、单体电池性能 Cell Performance----------------------------------  4

4、环境适应性 Environmental Function------------------------------6

5、安全性 Safety Tests--------------------------------------------  8

6、测试条件 Test Conditions----------------------------------------9

7、储存及其它事项 Storage and Others-------------------------------10

8、保质期及产品责任 Warranty Period& Product Liability-------------10

9、警告 Caution----------------------------------------------------10

10、免责声明Free-ResponsibilityDeclaration--------------------11

11、附录Appendix----------------------------------------------11

1、适用范围Scope

本规格书描述的电池组产品适用于小型后备/移动电源、电动车、电动摩托 车、汽车领域。

2、电池组特性BatteryGroupSpecifications

| 电芯 Cell | 容量Capacity(0.5C) |  | 15Ah |
| --- | --- | --- | --- |
|  | 标称电压RatedVoltage(V) |  | 3.2V |
|  | 典型内阻TypicalImpedance(mΩ) |  | ≤2mΩ |
|  | 电池材料 BatteryMaterial |  | LiFePO4 磷酸铁锂 |
| 电池组 PACK | 组合方式CombinationMethod |  | 4S2P |
|  | 最小容量MinimalCapacity(0.5C) |  | ≥30Ah |
|  | 额定电压NominalVoltage |  | 12.8V |
|  | 最大充电电压Max.ChargeVoltage |  | 14.6V |
|  | 放电截止电压DischargeCut-offVoltage |  | ≤8V |
|  | 最大充电电流MaxChargeCurrent |  | 30A |
|  | CCA冷启动电流ColdStartCurrent |  | 1000 |
|  | 电池组内阻标准PackImpedanceStandard |  | ≤2.0mΩ |
|  | 电池重量Weight(Approx.) |  | 参考样品Around 4.5kgs |
|  | 最大外形尺寸Max.Dimension(L×W×H) |  | 168*127*177mm |
|  | 适用温度 OperatingTemperature | 充电ChargeTemperature | 0℃～55℃ |
|  |  | 放电DischargeTemperature | -10℃～65℃ |
| 保护板 Protection Board | 单只过压保护值Single cellover-charge cut-off voltage |  | 3.8V |
|  | 过压释放值over-chargereleasevoltage |  | 3.65V |
|  | 单只欠压保护值Singlecellunder-discharge cut-offvoltage |  | 2V |
|  | 欠压释放值Dischargereleasevoltage |  | 2.2V |
|  | 过流保护值Over-dischargecut-offcurrent |  | 800A |
|  | 过流保护延时Over-dischargecut-offcurrent delay |  | No(无) |
|  | 短路保护Short-circuitprotection |  | Yes(是) |
|  | 短路保护延时Short-circuitprotectiondelay |  | No无 |
|  | 过流\短路保护恢复条件 Condition for the recovery of over-current and Short-circuit |  | No(无) |
|  | 均衡电流Balancecurrent |  |  |
|  | 均衡开启BalanceCondition |  | 无 |
|  | 通信协议 |  | 无 |

3、电池组性能Battery PackPerformance

| 项目Items | 测试方法Test Methods | 合格标准 Acceptancecriteria |
| --- | --- | --- |
| 3.1低温放电容量 Dischargecapacity at -10°C | 电池按照6.1规定方法充电后，在-10℃±2℃下贮存 26~28h，然后在-10℃±2℃下，以 0.5 C放电至 终止电压。 Step 1: The battery shall be charged inaccordancewith6.1. Step2:The battery shall be stored，inanambient temperature of −10℃±2℃，for not less than 26h and not more than 28h. Step3:Thebattery shall be discharged, in anambienttemperature of −10℃±2℃， at aconstant current of 0.5 C，until its voltage is equal tothespecified end-of-discharge voltage. | 放电容量/标称容量 ×95% Discharge Capacity/Nominal capacity×95% 0.5C:≥70% |
| 3.2高温放电容量 Discharge capacity at 55 °C | 电池按照6.1规定方法充电后，在55℃±2℃下贮存30-40h，然后在55℃±2℃下，以 0.5 C放电至终止电 压。 Step 1: The battery shall be charged in accordance with 6.1. Step 2: The battery shall be stored, in an ambient temperature of 55℃±2℃。 Step 3: The battery shall be discharged，in Anambienttemperature of 55℃±2℃，ata constant current of 0.5 C， until its voltage isequalto the specified end-of-dischargevoltage. | 0.5C:≥95% |
| 3.3倍率性能 Highratedischarge performance at 20 °C | 电池按照6.1规定方法充电后，在20℃±5℃搁置1~4小时，然后在 20℃±5℃的环境下，以0.5C/ 1.0 C放电至终止电压。 Step 1:The cell or battery shall be chargedinaccordance with 6.1. Step 2:The cell orbatteryshall bestored， in an ambient temperatureof20℃±5℃，for not less than 1 h and notmorethan 4h. Step 3:The cell or battery shall bedischarged，inan ambient temperature of 20℃ ±5℃， ataconstant current of 0.5C/ 1.0 C， until its voltageisequal to the specified end-of-dischargevoltage. | 0.5C:≥100％ 1C:≥95％ |

| 3.4荷电保持/恢复能力 Charge retentionandrecovery | 电池按照6.1规定方法充电后，在20±2℃的环境下贮存28天。再以0.5 C放电至终止电压。放电后的电池在24h内按照6.1充电，然后在20±2℃的环境下保存1~4小时，再以0.5C放电至终止电压。 Step 1: The battery shall be charged inaccordancewith 6.1. Step 2: The battery shall be stored inanambient temperature of 20℃±5℃， for28days. Step 3: The battery shall be discharged，inan ambient temperature of 20℃±5℃，ataconstantcurrentof0,5C，untilitsvoltageisequalto the specified end-of-dischargevoltage. Step 4: The battery shall then be chargedinaccordance with 6.1， within 24 h followingthedischarge of step 3. Step 5: The cell orbatteryshall be stored， in an ambient temperatureof 20℃±5℃， for not less than 1 h and notmorethan 4 h. Step 6: The cell or battery shallbedischarged， in an ambient temperature of 20℃±5℃，at a constant current of 0.5 C， untilitsvoltage is equal to the specifiedend-of-dischargevoltage. | 0.5C:≥95％ |
| --- | --- | --- |
| 3.5存储性能 Chargerecovery afterstorage | 电池按照6.1规定方法充电后，在 20℃±2℃下，以0.5 C 放电60分钟，然后在 20℃±2℃下贮存 90天。电池按4.1方法充电，搁置1~4小时，然后在 25℃±2℃下，以0.5 C 放电终止电压。充放电循环允许进行5次。 The battery shall be charged in accordance with6.1. The battery shall be discharged，in anambient temperature of 20℃±5℃，at aconstant current of 0,5 C，for 60min. The battery shall be stored in an ambienttemperature of 20℃±2℃，for 90 days. The battery shall be charged，in an ambienttemperature of 20℃±5℃，in accordance with6.1.The battery shall be stored，in an ambienttemperature of 20℃±5℃，for not less than 1h and not more than 4 h. Thebattery shall be discharged，in an ambienttemperature of 20℃±5℃，at a constantcurrent of 0.5 C，until its voltage is equal to the specified end-of-discharge voltage. Charge-discharge cycle may be repeated up to four additional times，as necessary to satisfy the requirement. | 0.5C:≥95％ |

| 3.6循环寿命 Endurance in cycles | 电池按照6.1 规定方法充电后，搁置 30min；0.3 C 恒流放电至放电终止电压；搁置 30min；按照上述 方法循环。当电池容量低于80%额定容量时停止。 Step 1: The battery shall be charged in accordance with 6.1. Step 2: The battery shall be stored in an ambient temperature of 20℃±2℃，for 30 min. Step 3:The battery shall be discharged，in an ambient temperature of 20℃± 5℃，at a constant current of 0,3 C， until its voltage is equal to the specified end-of-discharge voltage. Step 4: The battery shall be stored in an ambient temperature of 20℃±2℃，for 30 min. Step 5:Repeat step 1 to 4， until the capacity of battery less than 80% of its rated capacity | ≥2000cycles |
| --- | --- | --- |

4、环境适应性 Environmental Function

| 项目Items | 测试方法Test Methods | 合格标准 Acceptancecriteria |
| --- | --- | --- |
| 4.1温度循环 Temperature cycling | 电池充满电后，按照下述步骤在强制通风箱中做温度 循环（-20℃~75℃）。 步骤 1：电池在75℃±2℃的环境温度下搁置4小时。 步骤 2：在30min内将温度降低到20℃±5℃，并保 持2小时。 步骤 3：在30min内将温度降低到-20℃±2℃，并保 持4小时。 步骤 4：在30min内将温度升高到20℃±5℃，并保 持至少2小时。 步骤 5：再重复上述步骤4个循环。 步骤6：第5次循环后，储存7天。 Fully charged batteries are subjected to temperature cycling (-20℃~+75℃) in forced draught chambers，according to the following procedure。 Step 1: Place the batteries in an ambient temperature of 75℃±2℃ for 4 h. Step 2:Change the ambient temperature to 20℃±5℃with in 30 min and maintain at thistemperature for a minimum of 2 h. Step 3: Change the ambient temperature to -20℃±2℃ within 30 min and maintain at this temperature for 4 h. Step 4: Change the ambient temperature to 20℃± 5℃ within 30 min and maintain at this temperature for a minimum of 2 h. Step 5: Repeat steps 1 to 4 for a further four cycles。After the fifth cycle，store the batteries for seven days prior to examination. | 不漏液 不起火 不爆炸 No Fire No Explosion NoLeakage |

| 4.2振动 Vibration | 电池充满电后，确认电池电压为满电状态。然后将电 池固定在振动台上，施加振幅为0.76mm的简谐振动， 总的最大偏移为1.52mm。电池以1Hz的速率，在频 率10Hz~55Hz~10 Hz间往复振动，总时间为 90±5min。电池在三个垂直的安装位置（振动方向） 上，分别振动一次。测试完成后，搁置1小时。 Fully charged batteries are vibration-tested under the following test conditions. Simple harmonic motion is applied to the batteries with amplitude of 0.76mm，and a total maximum excursion of 1.52mm. The frequency is varied at the rate of 1 Hz/min between the limits of 10 Hz and 55 Hz. The entire range of frequencies (10 Hz to 55 Hz) and return (55 Hz to 10 Hz) is traversed in 90min±5min for each mounting position (direction of vibration). The vibration is applied in each of three mutually perpendicular directions，in the sequence specified below. Step 1: Verify that the measured voltage is typical of the charged product being tested. Steps 2-4: Apply the vibration as specified in Table. Step 5: Rest battery for 1 h, then make a visual inspection. | 不漏液 不起火 不爆炸 No Fire No Explosion NoLeakage |
| --- | --- | --- |
| 4.3低压 Low Pressure | 电池充满电后，放置到20℃±5℃的真空箱中。将真空箱的压力逐渐降低到11.6 kPa，保持6小时。 Each fully charged is placed in a vacuum chamber in an ambient temperature of 20 ℃± 5 ℃. Once the chamber has been sealed，its internal pressure is gradually reduced to a pressure equal to or less than 11.6 kPa held at that value for 6 h. | 不漏液 不起火 不爆炸 No Fire No Explosion NoLeakage |

5、电芯安全性 Cell Safety Tests

| 5.1自由跌落 FreeFall | 充满电的电池从 1.0m 高度自由跌落到水泥地面上 3次，方向随机。 Each fully charged battery is dropped three times from a height of 1.0 m onto a concrete floor。 The batteries are dropped so as to obtain impacts inrandom orientations. | 不漏液 不起火 No Fire No Explosion |
| --- | --- | --- |
| 5.2机械冲击 MechanicalShock | 将充满电的电池固定在测试机器上进行冲击测试。电池要承受等值的三次冲击，在相互垂直的三个方向上各进行一次。其中至少有一个方向应当和电池的最大平面垂直。电池承受冲击的加速方式：在最初 3ms内，最小平均加速度为 75 gn，峰值加速度应在 125 gn和 175 gn 之间。电池应在 20℃±5℃的环境下进行测试。 The fully charged battery is secured to the testingmachine by means of a rigid mount which will support all mounting surfaces of the battery. Thebattery is subjected to a total of three shocks of equal magnitude. The shocks are applied in eachof three mutually perpendicular directions. At leastone of them shall be perpendicular to a flat face. For each shock the battery is accelerated in such amanner that during the initial milliseconds theminimum average acceleration is 75 gn. The peakacceleration shall be between 125 gn and 175 gn. Batteries are tested in an ambient temperature of 20℃±5℃. | 不漏液 不起火 No Fire No Explosion |
| 5.3挤压 Crushing ofCells | 将充满电的单体电池放置在 20℃±5℃条件下，挤压方向：垂直于蓄电池极板方向施压；挤压头面积：不小于 20c ㎡；挤压程度：直至蓄电池壳体破裂或内部电路（蓄电池电压为 0V）。 Put the fully charged single cell in the condition of 20℃±5℃.Extrusion direction: Pressure on the direction ofperpendicular to the battery plate. Extrusion size: not less than 20 c ㎡. Extrusion Level: until the battery case rupture orthe internal circuit (battery voltage is 0V). | 不爆炸 不起火 No Fire NoExplosion |
| 5.4过充电 Overcharge | 单体电池以 0.5 C 放电到终止电压，然后使用 3.65V 的充电器，以 0.2C 电流充电 12.5 小时。 The cell is discharged with 0.5 C to theend-of-discharge voltage，then charged from apower supply of 3.65 V，at the charging current 0.2 Cfor 12.5 h. | 不爆炸 不起火 No Fire NoExplosion |
| 5.5 过放电 Forced Discharg | 电池在20℃±5℃下，以0.5C电流放电（如果有电子保护线路，应暂时除去放电电子保护线路），直至某一单体电池电压达到 0V 结束试验。 20℃±5℃, 0.5C discharge. (If has electronic protection circuits, the electronic discharge protection circuit should be temporarily removed), tests ends until a single battery voltage reaches 0V. | 不爆炸 不起火 No Fire NoExplosion |
| 5.6针刺 Acupuncture | 用φ3mm-φ8mm 的耐高温钢针、以 10mm/s-40mm/s 的速度，从垂直于蓄电池极板的方向贯穿（钢针停留在蓄电池中）。 Prong it by direction of perpendicular to the battery,with φ3mm-φ8mm high thermal resistant needle bythe speed of 10mm/s-40mm/s.(the steel needle stayon the battery) | 不爆炸 不起火 No Fire NoExplosion |

6、测试条件Test Conditions

除非另有说明，所有测试都应在静止空气中进行。

Unless otherwise stated，all tests that are described in this clause shall be performed in still air.

6.1充电方法 ChargeProcedure

充电前，电池应在20℃±5℃的初始温度下以0.5C恒流放电到放电终止电压。除非另有说明，电池应在20℃±5℃初始温度下，以0.2 C恒流，以(3.60V*N)限压充电到电流降至0.02C结束。

Prior to charging，the battery shall be discharged at 20℃±5℃ at aconstantcurrentof 0.5 C，down to the specified end-of-dischargevoltage.Unless otherwise stated，the battery shall be charged at constant current 0.2 Candlimited volt at 3.60V*N，then end until the current downto 0.02C.

6.2环境Ambient

温度/Temperature：20±5℃

湿度Humidity：25-85﹪RH

大气压/Air pressure：86KPa～106kPa

7、 储存及其它事项 Storage and Others

7.1 长期储存LongTimeStorage

长期储存的电池（超过 3 个月）须置于干燥、凉爽处，每 6个月对电池进行一次充放电。If the cell is stored for a long time(exceed three months)，the cell should be storedindrying and cooling place The cell should be charged and discharged eachsixmonths.

7.2 其它事项Others

本规格书中未提及的事项，须经双方协商确定。Anymattersthatthisspecificationdoesnotcovershouldbecoveredbetweenthecustomer.

8、 保质期及产品责任 Warranty Period& Product Liability

8.1保质期是从出厂日期（喷码/标示）开始起，质保期在销售合同中另定；Warranty period begins from the delivery date， and is exclusively made in thesalecontract.

8.2若不按说明书中的预防措施操作而引发事故，本公司将不承担责任。will not be responsible for any accidents caused by not following theprecautionmethods ordirections.

8.3如果保质期内发生的问题不是由于本公司的生产过程造成的或是由于客户本身滥用或使用不当造成的，本公司将不会无偿包换。Problems arise not caused by our production process，but due tocustomers’negligence or improper usage， we will not be responsible for anyreplacements.

8.4当本规格书版本更新时。When the specification ismodified.

9、警告 Caution

9.1不要拆解电池。

Donot dismantle， open or shred thebatteries.

9.2 电池应远离热源、火源，避免阳光直射。

Donotexposebatteriestoheatorfire。Avoidstorage in direct sunlight.

9.3 不要短路电池，避免将电池放置在容易引起短路的地方。

Do not short-circuit the battery，Do not store batteries haphazardly in a box or drawer where they may be short-circuited by other metal objects.

9.4 充电口和放电口绝对不能混用，否则有可能发生安全事故。

Forbid confusedly using the charge socket and discharge socket， or accidents may occurred。

9.5 避免电池受到冲击。

Do not subject batteries to mechanical shock.

9.6 电池发生泄漏时，避免电解液接触皮肤和眼睛。如果发生接触，立即用大量水冲洗；情 况严重时应及时就医。

In the event of a cell leaking，do not allow the liquid to come in contact with the skin or eyes. If contact has been made，wash the affected area with copious amounts of water and seek medical advice.

9.7 连接时确保电池正负极和用电器正负极一致，避免反接。

Observe the plus (+) and minus (-) marks on the battery and equipment and ensure correct use.

9.8将电池放置在儿童不宜接触的地方。Keep batteries out of the reach ofchildren.

9.9电池应保持清洁、干燥。Keep batteries clean anddry.

9.10 电池端子变脏时，可用干布擦拭。

Wipe the battery terminal s with a clean dry clothifthey becomedirty.

9.11电池使用前要先进行充电，应采用厂家指定的充电器按照用户手册说明充电。

Batteriesneed to be charged before use. Always use the correct charger and refer tothemanufacturer’s instructions or equipment manual for proper charginginstructions.

9.12 电池不使用时，不要长时间充电。

Donotleaveabatteryonprolongedchargewhennotinuse.

9.13 电池经长时间储存后，经过几次充电和使用，性能会恢复最好。

After extendedperiodsof storage， it is necessary to charge and discharge the batteries several timestoobtain maximumperformance.

9.14 电池在室温(20℃±5℃)下性能最好。

Thebatteriesgivetheirbestperformancewhenthey are operated at normal room temperature (20℃±5℃).

9.15 保留说明书以作后续使用参考。

Retain the original product literature forfuturereference.

9.16 电池不能作别的用途使用。

Use only the battery in the application for which itwasintended.

9.17 电池长时间不用时，需要从用电器上取下。

Whenpossible，removethebatteryfromthe equipment when not inuse.

9.18 电池不要随意丢弃。Dispose ofproperly.

9.19电池做为电摩或其它备用电源使用时，要与负载的控制器或装置配套使用；因电池组配有保护电子线路，不可直接驱动纯电感负载，否则会损坏系统。

Cells used as E-motor or storage power should be matched with controller orrelatedequipment. Becausethebatterypilesarematchedwithprotectionboard，youcannotdrivethepureinductanceequipmentotherwiseyoucoulddamagethewholesystem.

10、免责声明Free-ResponsibilityDeclaration

产品使用前，请用户说细阅读产品规格书、使用说明书及使用注意事项等，了解产品的 使用方法及应用范围；若出现产品使用方法错误、电路连接不对或采用的输入电源、负 载功能参数与产品规格书所标性能参数不符等现象均属使用不当，由使用不当造成产 品、负载及周边连接件的损坏，本公司均不承担任何责任。

Before using the battery，you should read the specifications，usage instructionandsome  attentionscarefully  to  learn  its  application  method  and  areas. If  the phenominon such as error using methodwrong circuit connection, or input power data，working index are inconsisted with the specifcations happen and cause damage to production，circuit and its accessories，we are not responsible for it.

11、附录Appendix